3 Layer knit fabric - Technical Specification

## Product Overview

3-layer softshell composite knit fabric with waterproof, windproof, water-repellent, breathable and stretchable performance, designed for outdoor apparel and work wear. It offers durable protection, long service life and comfortable wearing experience.

## Material Composition

- Face fabric: 100% polyester interlock knit

- Middle layer: PU elastic thin membrane

- Back fabric: 100% polyester mesh

## Key Performance Parameters

### Water Resistance

- Test standard: JIS L1092B

- Result: 10,000 mm

### Moisture Vapor Permeability

- Test standard: JIS L1099B1

- Result: 10,000 g/m²·24h

### Water Repellency

- Before washing: 90 points

- After 5 washes: 80 points

### Basic Physical Properties

- Weight: 237 g/m²

- Width: 56 inches

- Finish: Piece dyed + water repellent treatment

## Features

- Waterproof

- Windproof

- Water repellent

- High moisture vapor permeability (breathable)

- Ultra-elastic

- 4-way stretch

- Abrasion resistant

- Durable

- Long service life

- Soft hand feeling & comfortable

## Applications

- Outdoor wear: vests, jackets, jumpsuits, pants, outdoor gear

- Sports wear: bike wear, ski wear, elite sports apparel

- Work wear & protective gears

## Order Requirements

- MOQ: 1000 yards