
3 Layer knit fabric - Technical Specification
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[bookmark: heading_0]Product Overview
3-layer softshell composite knit fabric with waterproof, windproof, water-repellent, breathable and stretchable performance, designed for outdoor apparel and work wear. It offers durable protection, long service life and comfortable wearing experience.
[bookmark: heading_1]Material Composition
· Face fabric: 100% polyester interlock knit
· Middle layer: PU elastic thin membrane
· Back fabric: 100% polyester mesh
[bookmark: heading_2]Key Performance Parameters
[bookmark: heading_3]Water Resistance
· Test standard: JIS L1092B
· Result: 10,000 mm
[bookmark: heading_4]Moisture Vapor Permeability
· Test standard: JIS L1099B1
· Result: 10,000 g/m²·24h
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· Before washing: 90 points
· After 5 washes: 80 points
[bookmark: heading_6]Basic Physical Properties
· Weight: 237 g/m²
· Width: 56 inches
· Finish: Piece dyed + water repellent treatment
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· Waterproof
· Windproof
· Water repellent
· High moisture vapor permeability (breathable)
· Ultra-elastic
· 4-way stretch
· Abrasion resistant
· Durable
· Long service life
· Soft hand feeling & comfortable
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· Outdoor wear: vests, jackets, jumpsuits, pants, outdoor gear
· Sports wear: bike wear, ski wear, elite sports apparel
· Work wear & protective gears
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· MOQ: 1000 yards

